## Greif Poland Technical Specification

## for the following bottles:

0-04-0770-6-00-000-X

Greif Poland Sp. z o. o.

Ul. Przemysłowa 3

44-203 Rybnik

tel. +48 32 42 95 040

fax. +48 32 42 95 041

## Greif Poland Technical Specification

## for the following bottles:

## 0-04-0770-6-00-000-X

- Requirements of quality.

- Marks on a bottle.

- Requirements of labelling.

- Labelling of packages, description of code.

- Producer’s recommendation.

- Nr of batch.

Ad. pkt. 1. Requirements of quality.

- Appearance:

- Clean, without damages and any contaminations.

- Neck processing, neck trimming, smooth upper and bottom joints.

- Blue colour, uniform, transparent, attachment no. 1a.

- Careful labels application.

- Dimensions:

- Bottle height 488 (+/ - 3 mm), attachment no. 1b.

- Bottle diameter 272 (+/ - 2 mm), attachment no. 1b.

- Bottle capacity 18,9l (+/ - 0, 25 %).

- Outside neck diameter 55, 30 (+/ - 0, 45), attachment no. 1b.

- Bottle weight 770g (+ / - 25 g.), attachment no. 1b.

# Ad. 2 Marks on a bottle.

# Attachment no. 2.

Ad. 3 Requirements of labeling.

- Attachment no. 3.

# Ad. 4 Labelling of packages, code explanations.

# Attachment no. 4.

Ad. 5 Producer’s recommendation.

- Attachment no. 5.

Ad. 6 Batch’s description.

- Bottles produced at the same time, on two separate production lines have different batch numbers.

- Bottles produced on one line, from the same Polycarbonate batch in a continuous way have the same batch number.

  - In case of stopping the production and restarting, a new batch number is assigned.

Attachment no.1a

Assesment criteria of bottles’ transparency

36-Not Approved

28 – Not Approved

24 – Not Approved

18 – Not Approved

16 – Not Approved

14 – Not Approved

12 – Approved

10 – Approved

8 – Approved

6 – Approved

Attachment no. 1b

Attachment no. 2

Marks on a bottle

Day of production

Month of production

Shift number

Year of production

Type of raw material

Mould number (e.g. 36/ 41/ 63/ 64/ 69/ 71)

Attachment no. 3

Attachment no. 4

Product no.: 0-04-0770-6-00-000- X Internal order no.: SFC 03808 Palette no: Batch 1 z 108 200001 Palette type: 27

Product no. (description):

- Type of material (Polycarbonate).

04- Bottle 18,9l. four ribs with handle.

0770- Bottle weight (decagram).

6- Neck type.

- Insert (catalogue number).

000- Label (catalogue number).

X - bottles in single packaging.

X - Packaging type:

0 – 9 bottles in single packaging

1 – 4 bottles in single packaging

2 – 8 bottles in single packaging

3 – 27 bottles in single packaging

4 – 52 bottles in single packaging

5 – 60 bottles in single packaging

6 – 88 bottles in single packaging

8 – 72 bottles in single packaging

9 – 18 bottles in single packaging

- - 9 bottles in single packaging

- - 4 bottles in single packaging

- - 8 bottles in single packaging

- - 27 bottles in single packaging

- - 52 bottles in single packaging

- - 60 bottles in single packaging

- - 88 bottles in single packaging

- - 72 bottles in single packaging

- - 18 bottles in single packaging

- - 9 bottles in single packaging

- - 4 bottles in single packaging

- - 8 bottles in single packaging

- - 27 bottles in single packaging

- - 52 bottles in single packaging

- - 60 bottles in single packaging

- - 88 bottles in single packaging

- - 72 bottles in single packaging

- - 18 bottles in single packaging

Internal order number e.g. SFC 03808.

Palette number e.g.. 1,2,3…of  108.

Palette type  e.g. 27.

Batch number e.g. 20001.

SFC 03808 Greif order number.

1,2,3…- Packaging number

108- Number of packaging within order.

27- Quantity of bottles in single packaging.

20001- Next batch number.

Attachment no. 5

DEAR CUSTOMER

We herby inform that Polycarbonate bottles purchased in Greif Poland should be disinfected and rinsed precisely before each use.

The washing and sterilizing detergents should have the proper certificates and should be used according to the procedures recommended by their producers.

Insert

Label

Type of packaging

Insert

Label

Type of packaging